## Slide 1
Yongdan Li
Professor of Industrial Chemistry
Department of Chemical and
Metallurgical Engineering
School of Chemical Technology
Aalto University
Email: Yongdan.li@aalto.fi
And
Adjunct Chair Professor of Industrial Catalysis
Tianjin University
Chemical and fuel commodities through catalytic solvolysis of lignin
A presentation on celebrating the 40th anniversary of CACS

## Slide 2: Contents
Background
Part 1: Ethanolysis of Kraft lignin
Part 2: Depolymerization of enzymatic hydrolysis lignin

## Slide 3
The next Grand Challenge
Global Carbon Imbalance
IPPC AR-4，2007
Nature carbon cycle (1750)
Human disturbance (the last decade of the 20th century)
6.4 billion tons of carbon (23.5 billion tons of CO2) are released annually

## Slide 4
Background
biomass
coal
natural gas
petroleum
others
hydroelectric
Biomass is enough for fuels and chemicals
＞
http://www.eia.gov/todayinenergy
Over 150 billion-tons annual supply
Development of biofuel is urgent
nuclear
biomass
Consumption in the USA, Quadrillion Btu
Notes: 千兆英热

## Slide 5
Background
Lignin, the only renewable aromatic resource
Nature 454, 841-845 (2008)
Low-heating-value fuel
13.5-15.5 MJ/kg
High value-added platform chemicals
Lignin
Hemicellulose
Cellulose

## Slide 6
Background
Lignin shows lower O/C, higher energy content among lignocellulosic biomass, indicating it is more promising as a petroleum alternative.
Schematic representation of a soft wood lignin structure
Chem. Rev., 2010, 110, 3552-3599

## Slide 7
Background
Chemicals
Platform chemicals
Materials
Polyurethane
Phenolic resin
Carbon fiber
High
Value
Low heating-value (ca. 13.5-15.5 MJ/kg)
High ash content Si, Ca, Mg, et al.
·
Fuels
Value added
Potential applications of lignin
Chem. Rev., 2015, 115, 11559-11624

## Slide 8
Background
Available lignin resources
Kraft Lignin
Enzymatic Hydrolysis Lignin
Byproduct of bio-ethanol
Organosolv Lignin
Soluble in organic solvent
Steam explosion lignin
Others
Oxidation lignin
Byproduct of pulping industry
Insoluble in water
Only Kraft lignin is produced in an industrial scale.
Enzymatic Hydrolysis Lignin probably become future major lignin raw stock

## Slide 9
Part 1.1: Ethanolysis of Kraft lignin over MoC1-x/AC

## Slide 10
Ethanolysis of Kraft lignin over MoC1-x/AC
APB
Arenes, phenols and benzyl alcohols
280 oC， 6 h
Ethanol，MoC1-X/AC
HAE
Higher alcohols and esters
HAE
APB
84 peaks related to Kraft lignin
52 peaks are qualified
25 peaks are quantified
32 peaks are still unknown
No char
Kraft Lignin
(Sigma)
Insoluble
Overall yield of quantified products 1.64 g/g lignin.
Angew. Chem. Int. Ed., 2014, 126, 7438-7443

## Slide 11
Ethanolysis of Kraft lignin over MoC1-x/AC
Angew. Chem. Int. Ed., 2014, 126, 7438-7443
  XRD pattern (A) and TEM image (B) of the α-MoC1-x /AC.

## Slide 12
Ethanolysis of Kraft lignin over MoC1-x/AC
Angew. Chem. Int. Ed., 2014, 126, 7438-7443
Alcohols – C6
25 main products cover 84% of the total area in the GC-FID
Esters – C8
Esters – C10
Benzyl alcohols
Phenols
Arenes
58.4%
25.2%
16.4%

## Slide 13
Ethanolysis of Kraft lignin over MoC1-x/AC
Angew. Chem. Int. Ed., 2014, 126, 7438-7443
Gas atmosphere：
As H2 increases, the yield decreases
Yield in N2 is higher than that in H2
Effect of initial PH2 on yield
Yields comparison in N2 & H2
3 4 5 6

## Slide 14
Ethanolysis of Kraft lignin over MoC1-x/AC
Angew. Chem. Int. Ed., 2014, 126, 7438-7443
Ethanol is the most efficient solvent for Kraft lignin conversion

## Slide 15
Part 1.2: Reaction mechanism

## Slide 16
Proposal of the reaction mechanism
SEM of lignin samples
Sample | SBET (m2/g) | VO (cm3/g) | Vm (cm3/g) | Pore diameter (nm)
MoC1-x/AC | 749 | 0.12 | 0.59 | 7.9
The pore diameter of MoC1-x/AC catalyst
Adsorption
×
Lignin Partical Size 20-80 μm >> Catalyst Pore Diameter 7.9 nm
Angew. Chem. Int. Ed., 2014, 126, 7438-7443

## Slide 17
Proposal of the reaction mechanism
MALDI-TOF-MS profiles of various substrates：
Kraft lignin treated in supercritical ethanol without catalyst,
(b) Kraft lignin treated in supercritical ethanol over the MoC1-x/AC catalyst.
Without a catalyst
With the MoC1-x/AC
Angew. Chem. Int. Ed., 2014, 126, 7438-7443
Large molecules disappeared

## Slide 18
Proposal of the reaction mechanism
ACS Catal., 2015, 5 , 4803–4813
Liquid product yields of lignin conversion over different Mo-based catalysts
The FT-IR spectra of the different samples before and after reaction
Mo-O stretching vibration
-CH3 and -CH2 stretching vibration
All the Mo-based catalysts show high and similar activities
A
B
Used MoO3/Al2O3, (b) Used Mo/Al2O3, (c) Used α-MoC1-x/AC, (d) Used Mo2N/Al2O3
(e) Kraft lignin, (f) Dried liquid product from lignin catalyzed by Mo/Al2O3.

## Slide 19
Proposal of the reaction mechanism
ACS Catal., 2015, 5 , 4803–4813
(A) Photographs of (a) used Mo/Al2O3 catalyst with liquid products, (b) fresh Mo/Al2O3 catalyst in ethanol in EPR sample cell.
(B) EPR spectra of (a) used Mo/Al2O3 catalyst, (b) fresh Mo/Al2O3 catalyst and (c) Kraft lignin.
paramagnetic Mo (V)
Other used Mo-based catalysts with g tensor around 1.92 were also recorded, indicating the presence of Mo (V)

## Slide 20
Proposal of the reaction mechanism
ACS Catal., 2015, 5 , 4803–4813

## Slide 21
Part 1.3: Ethanolysis of Kraft lignin over MoC1-x/Cu-MgAlOz

## Slide 22
Ethanolysis of Kraft lignin over MoC1-x/Cu-MgAlOz
CuMgAlOy
MoC1-x/Cu-MgAlOz
(NH4)6Mo7O24
impregnation
CuMgAl-Quintinite
CuMgAlOy
MoC1-x/Cu-MgAlOz
Appl. Catal. B, 2017, 202, 305-313
H2/CH4
TPR

## Slide 23
Ethanolysis of Kraft lignin over MoC1-x/Cu-MgAlOz
Appl. Catal. B, 2017, 202, 305-313
Activity of CuMgAlOy increased after reduction.
Roles of components in catalyst
Catalysts
MoC1-x/AC is more active.
Physical mixture catalyst is better than either.
The combined catalyst shows the best activity.

## Slide 24
Ethanolysis of Kraft lignin over MoC1-x/Cu-MgAlOz
Appl. Catal. B, 2017, 202, 305-313
Highest Yield：3207 mg/g lignin
Aromatics 575 mg/g lignin
Alcohols 704 mg/g lignin
Esters 1928 mg/g lignin
As temp. increased，the yield rise
successive run for 5 times
（330 oC, 6h）
24

## Slide 25: Summary of Kraft lignin ethanolysis over Mo-based catalysts
Complete catalytic ethanolysis of Kraft lignin to alcohols, esters and aromatics over MoC1-x/AC with a yield of 1.64 g/g lignin.
Ethanol itself depolymerizes Kraft lignin. The dissociative Mo (V) ethoxide facilitates the complete decomposition of the segments. Ethanol pieces are incorporated into the product molecules.
The combination of MoC1-x and Cu-MgAlOz maximizes the catalytic activity.
25

## Slide 26
EHL
Bio-ethanol
EHL
Energy Fuels 2017, 31, 7223−7233
(EHL)
Gasoline, jet fuel and diesel
Catalyst
An emerging topic:
Catalytic solvolysis of enzymatic hydrolysis lignin (EHL)

## Slide 27
EHL
Lignin source: Corn stover
Chart: 
| Lignin | Ash
Content | 0.912 | 0.088
C | H | N | S | O
61.75% | 6.48% | 0.90% | 0.58% | 30.29%
Elemental analysis of EHL
2D-HSQC of EHL
Notes: The EHL has high purity and low content of sulfur (Others：: Ash, and residual carbohydrate )
EHL contains different ether linkages (A,B,C) and different type primary monomers,
sinapyl (S), coniferyl (G), and p-coumaryl (H) alcohols as well as p-coumaric acid (pCA) and ferulic acid (FA)

## Slide 28
Part 2.1: Catalytic ethanolysis of EHL without H2

## Slide 29
No tar or char is formed, and the EHL is completely liquified
Complex alkylphenols are the main products
WO3/γ-Al2O3 catalyzed EHL ethanolysis at 320 oC under 0 bar N2
Ind. Eng. Chem. Res. 2019, 58, 10255-10263
Catalytic ethanolysis of EHL without H2
31.6 wt% yields of monomers
Notes: In EHL ethanolysis without H2, WO3/γ-Al2O3 was used as catalyst,
After reaction, no tar or char is formed, and the EHL is completely liquified. Complex alkylphenols are the main products

## Slide 30
Ind. Eng. Chem. Res. 2019, 58, 10255-10263
Entry | Catalyst | Solvent | Yield (mg/g EHL) |  |  | 
 |  |  | Aromatic Ethers | Aromatic Esters | Phenolic Compounds | Overall Aromatic Compounds
1 | WO3 | Ethanol | 51.1 | 43.6 | 123.3 | 218.0
2 | H2WO4 | Ethanol | 23.1 | 11.5 | 128.3 | 169.1
3 | γ-Al2O3 | Ethanol | 19.3 | 2.4 | 43.7 | 65.5
4 | WO3/γ-Al2O3 | Ethanol | 32.9 | 26.3 | 245.2 | 315.8
5 | WO3/γ-Al2O3 | Methanol | 16.2 | 3.5 | 160.2 | 179.6
6 | WO3/γ-Al2O3 | Isopropanol | 26.8 | 5.7 | 96.0 | 128.2
Product yield and distribution over different catalysts
The WO3/γ-Al2O3 catalyst gave highest yield
Ethanol gave higher aromatic product yield than other alcohols
Catalytic ethanolysis of EHL without H2
Notes: Compare to WO3, H2WO4 and Al2O3, The WO3/γ-Al2O3 catalyst gives highest yield
Ethanol gives higher aromatic product yield than other alcohols

## Slide 31
Part 2.2: Catalytic ethanolysis of EHL with H2

## Slide 32
Ind. Eng. Chem. Res. 2020, 59 (16), 7466-7474.
220 oC
H2
Ni (220H)
Catalyst preparation: Nickel formate decomposition
Catalytic ethanolysis of EHL with H2
Part 2. Unsupported Ni catalyst catalyzed EHL ethanolysis with H2
Nickel formate
Ni Catalyst
XRD
TEM
Only Ni peaks
Notes: In EHL ethanolysis with H2, Unsupported Ni catalyst was used. This catalyst was prepared through nickel formate decomposition

## Slide 33
Fig. 5. Total-ion chromatogram (TIC) of the liquid product obtained from EHL depolymerization over Ni (220H) in ethanol over Ni (220H) at 280 oC for 6 h with 2 MPa H2.
Catalytic ethanolysis of EHL with H2
28.5 wt% yields of monomers
High yields of esters were detected
The alkylphenols only contain para-alkyls
Notes: After the reaction at at 280 oC for 6 h with 2 MPa H2, 28.5 wt% yields of monomers were obtained,
high yield of esters were detected and the alkylphenols only contain para-alkyls

## Slide 34
Ind. Eng. Chem. Res. 2020, 59 (16), 7466-7474.
Catalytic ethanolysis of EHL with H2
Effect of the solvent on the structure of main monomers.
TIC of products and structures of main monomers obtained from EHL depolymerization with Ni (220H) at 280 oC for 6 h with 2 MPa H2.
Methanol
Ethanol
Isopropanol
Notes: The reactions in different solvents indicated that the structures of aromatic esters were dependent on the solvent used, while the structures of para-alkyl phenols obtained in different solvent were same

## Slide 35
Ind. Eng. Chem. Res. 2020, 59 (16), 7466-7474.
Catalytic ethanolysis of EHL with H2
Formation of esters and para-alkylphenols
The conversion of primary monomers over Ni (220H) at 280 oC for 6 h
FA and pCA
G and S
esters
para-alkylphenols
FA
G
Notes: The conversion of two primary monomers were examined to reveal the formation of esters and para-alkylphenols
FA produces esters and para-ethyl phenol
G produce para-propanol substituted phenols, para-propyl and para-ethyl phenols
Therefore,
Esters formed from esterification of acid units (FA and pCA ) in EHL with solvent
para-alkyl side chains of phenols formed from the side chains of primary monomers in EHL

## Slide 36
Cleavage of linkages in EHL (2D-NMR analysis)
Catalytic ethanolysis of EHL with H2
Ether linkages can be cleaved without catalyst
C-C linkages in C’ are gradually cleaved during Ni(220H) catalyzed reaction
280 oC for 6 h with 2 MPa H2.
Ni(220H) catalyzed EHL depolymerization.
Notes: The liquid products obtained from EHL depolymerization were analyzed with 2D-NMR
Without catalyst, the ether linkages in EHL were completely cleaved after reaction at 280 oC for 6 h with 2 MPa H2, but the signals of C-C linked structure (C’) were detected.
The signals of C’ were generally weakened in Ni catalyzed reaction with the increase of reaction temperature and time

## Slide 37
Part 2.3: The effect of solvent for EHL depolymerization

## Slide 38
The effect of solvent for EHL conversion
Reaction condition: 320 oC, 27.6 bar H2, 7.5 h, ethanol solvent, NiMo/γ-Al2O3
Complex alkylphenols were the main products
25.5 wt% yields of monomers
NiMo/γ-Al2O3 catalyzed depolymerization of EHL in ethanol
Energy Fuels, 2019, 33, 8657-8665.
Notes: NiMo/γ-Al2O3 was used to depolymerize EHL
In ethanol, Complex alkylphenols were the main products

## Slide 39
The benzene rings in products was completely hydrogenated
The O in products was completely removed
Bioresource Technology 323 (2021) 124634
The effect of solvent for EHL conversion
Same reaction condition: 320 oC, 27.6 bar H2, 7.5 h, ethanol solvent, NiMo/γ-Al2O3
NiMo/γ-Al2O3 catalyzed depolymerization of EHL in cyclohexane
Products Yields
Total: 10.4 wt%
1.5 wt%
4.6 wt%
0.3 wt%
3.3 wt%
0.2 wt%
0.4 wt%
Notes: In cyclohexane, with the same catalyst under the same reaction condition
The benzene rings in products was completely hydrogenated andhe O in products was completely removed
Only cycloalkanes were detected.

## Slide 40
The product distribution strongly depends on the solvent, catalyst, with or without hydrogen.
In WO3/γ-Al2O3 catalyzed reaction without H2, complex alkylphenols are the main products. In Ni catalyzed reaction with H2, esters and para-alky phenols are the main products.
EHL was depolymerized into phenolic monomers in ethanol, but produced cycloalkanes in cyclohexane.
Summary: EHL catalytic depolymerization

## Slide 41
EU Horizon 2020 project 101006744 EHLCATHOL website: www.ehlcathol.eu; Welcome to join us!
Since 2010, the research on lignin chemical conversion has received funding from:
Ministry of Science and Technology of China
Natural Science Foundation of China
Ministry of Education of China
China Scholarship Council
European Union's Horizon 2020 research and innovation program under grant agreement no 101006744

## Slide 42
Congrats for the 40th Anniversary of CACS!
Let us expect a prosperous future!