## Slide 1
TiO2 nanotubes/Ti foil:
As functional supports and flexible electrodes in solar energy storage
PhD: Xuelan Hou
Prof. Peter D. Lund, Prof. Yongdan Li
Aalto University
Notes: PAPER ID: 3590931 PAPER TITLE: TiO2 nanotubes grown on Ti foil: As functional supports and flexible electrodes DIVISION: Division of Energy and Fuels SESSION: Electrochemistry-Enable Catalysis for Energy, Chemicals, & Materials SESSION TIME: 2:00 PM - 4:00 PM PRESENTATION FORMAT: Oral - Virtual ROOM & LOCATION: Virtual Room PRESENTATION DATE & TIME: Tuesday, 8/24/2021, 3:15 PM - 3:40 PM

## Slide 2
1
Introduction
2
3
Why choose the topic?
Our research work
Anode
Cathode
Conclusions
Outline

## Slide 3
1
Introduction

## Slide 4
History

## Slide 5
Why black titania ?
Fig. 1. A schematic diagram of the properties, preparation methods and applications of black TiO2

## Slide 6
Fig. 2. (a) A schematic diagram of a electrochemical set-up and the anodic growth of TNT a Ti metal sheet .1 (b) The parameters to tune the morphology of TNT by the anodic oxidation method.1 (c) Cross-sectional view of SEM of anodic TNT2
Why anodic TiO2 nanotube?
Electron density 3-4 :
TiO2 NPs: 7.67*1017 cm-3
Black TiO2 NPs: 5.61*1019 cm-3
|3.Energy Environ. Sci., 2013, 6, 3007–3014
4. J. Mater. Chem. A, 2014, 2, 8612-8616
t, C,V, T
(a)
(b)
(c)
TNTs : 1.24*1019 cm-3
B-TNTs : 5.55*1021 cm-3
Fig. 3. Schematic of electron pathway in TiO2 NPs and TNT
2. Chemical Engineering Journal, 2021, 131415.
1. Nanoscale. 2010;2(1):45-59.

## Slide 7
2
Our research work
Anode
Cathode

## Slide 8
Photoanode: Part I
(c)
(d)
(e)
(a)
(b)
Applied Catalysis B: Environmental 258 (2019): 117949.
Notes: 0.71, 1.44, 2.05and 1.73 mA/cm2,

## Slide 9
Multi-length scale effect on PEC efficiency:
Photoanode：Part Ⅱ
Photocurrent density :
Pure TNT: 0.05 - 0.5~1.0 mA/cm2 at 1.23 VRHE
10~50 times
Scale-up
Chemical Engineering Journal (2021): 131415.
A span 6 orders magnitude length scales ranging
from 10−8 m to 10−2 m
1 cm2 2 cm2 4 cm2 6 cm2

## Slide 10
a
b
c
d
Fig. (a) Normalized transient i-log(t) curves under 60 V in 50 ml electrolyte.(b). LSV curves (c) ABPE curves (d) Effect of six size factors on the photocurrent density at 1.23 VRHE under 100 mW/cm2 in 1 M NaOH. The numbers of the Y-axis multiply the minus orders specified in the insets are the size values.

## Slide 11
Scheme 1: the photon capture, charge carrier flow
and water splitting mechanism.
Mechanism
Chemical Engineering Journal (2021): 131415.

## Slide 12
(Photo)cathode
Electrochemical potentials of possible HER, CO2 RR and NRR in aqueous solution
for the production of different solar fuels.
J= -100 mA/cm2
Notes: 0.71, 1.44, 2.05and 1.73 mA/cm2,

## Slide 14
Lignin depolymerized products
Dye sensitized solar cell
Y123

## Slide 15
3
Conclusions

## Slide 16
Conclusions
1
2
4
Anodic TNT array is promising for the design of flexible and efficient (photo)electrode in electrochemical cells.
Multi-length scale effect shows importance on PEC water splitting cell .
Electrochemical reduction method, i.e. TAR, provides an operational control and time-saving pathway for preparation of black TNT.
3
Black TiO2 offers a platform for solar energy storage and electricity storage systems.

## Slide 17
Prof. Yongdan Li
Aalto University
Email : yongdan.li@aalto.fi
Link: https://people.aalto.fi/yongdan.li
Group link: https://www.aalto.fi/en/
department-of-chemical-and-metallurgical-engineering/industrial-chemistry

## Slide 18
Prof. Peter D. Lund
Aalto University
Email : peter.lund@aalto.fi
Link: https://people.aalto.fi/peter.lund#contact
Group link: https://physics.aalto.fi/en/groups/newergy/

## Slide 19
Thanks!
The China Scholarship Council (CSC), No. 201706250038
The Start-up Package of T10108 Professorship offered by Aalto University to Y. Li
Aalto University School of Science Project T30404
The Academy of Finland Flagship Program, Photonics Research and Innovation (PREIN), No. 320167